# System  COR-3500 THERMAL BREAK

Supply and fitting of hinged euro groove windows/doors comprising of 6063 aluminium alloy profiles with T5 thermal treatment.

The frame and sash are 55 mm & 63 mm deep respectively both in windows as in doors.  The average aluminium profile wall thickness is 1.5 mm. in  windows and 1,7 mm. in doors.

The aluminium profiles are provided with a thermal break which is achieved by inserting 24 mm wide 6.6 polyamide isolation strips which are reinforced with 25% fibre glass.

Classifications achieved at test centre*:

Air permeability according to EN 12207:2000		Class  4

Water tightness according to EN 12208:2000 		Class  E1200

Wind resistance according to EN 12210:2000		Class  C5

* Test reference 1,20 x 1,20  m. 2 Sashes

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.