# System COR-GALICIA PREMIUM with THERMAL BREAK

Supply and fitting of hinged windows and doors comprising of 6063 aluminium alloy profiles and T5 thermal treatment that are joined to timber mouldings.

The frame and sash are 66.4 mm & 85.3 mm deep respectively both in windows as in doors. The average aluminium profile wall thickness is 1.5 mm for windows and 1.6 mm for doors.

The aluminium profiles are provided with a thermal break which is obtained by inserting 14,6 mm and 16 mm. wide tubular polyamide 6.6 isolation rods that are reinforced with 25% fibre glass and polyolefin foam placed around the perimeter of the glazing space.

The joining of the external aluminium frames and the internal timber mouldings can be carried out in two ways: by fixing independently with clips and by way of assembly using an EPDM gasket.  In both cases, this assembly ensures a perfect absorption of the different material expansions

Weather tightness is achieved with a triple EPDM gasket.

Classifications achieved at test centre*:

Air permeability according to EN 12207:2000		Class  4

Water tightness according to EN 12208:2000 		Class  9A

Wind resistance according to EN 12210:2000		Class  C5

* Test reference 1,23 x 1,48  m. 2 Sashes.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.