# System VERANDA - SKYLIGHT

Supply and fitting of profiles for a veranda or skylight comprising of general modules of …………in dimension and made up of ……….. dividing areas using profiles in 6063 alloy with T5 thermal treatment.

A Load bearing structure comprising of ………. mullions type COR-9200 with a seen surface of 65 mm that ensures perfect resistance to bending when subject to wind action and ……… transoms type COR-9201 with a seen surface of 65 mm and includes drainage and ventilation channels and joined by using end caps that include expansion gaskets at both ends of the profile.

The glazing is carried out based on profile ref. COR-9206 that compresses around the perimeter to the glass and fixing it to the load bearing structure.  Finally over this, and in order to hide the screws, profile ref. COR-9214 is fitted resulting in a seen external aluminium surface of 65 mm.

Optimum weather tightness is achieved by using a triple barrier made up from EPDM gaskets.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.